## Slide 1
PIGMENTS ESRF BAG training with FullProf
program
1- generalities on X ray diffraction and Rietveld analysis
2- preparing the pcr command file
3- running FullProf: analysis of a ID22 SD pattern of hydrocerussite Pb3(CO3)2(OH)2
4- size / strain determination with the Williamson-Hall method
5- semi-quantitative phase analysis on Renaissance masters’ paintings
6- preferred orientation effects

## Slide 2
profile
→ microstructure
Bragg angle
→ lattice
intensity
→ atoms, phases amounts
1- information given by XRD

## Slide 3
1- the Rietveld analysis (1969)
a full-profile matching method for powder diffraction patterns
intensity yi at point 2i is a function of:
intensity
- % of the phase
- atomic positions
- occupation rate
- atomic displacement
- preferred orientations
lattice
- a, b, c, α, , γ
- h, k, l
- lattice mode
profile
- shape
- width
- microstructure
principle: - the intensity for each point (2i, yi) is the result of one equation
- least-square refinement of the variables
 minize χ2 = Σi wi (yi obs - yi calc)2 wi = 1/σ2(yi obs)
Hugo Rietveld (1987)
High-Flux Reactor, Energy Research Foundation
Petten, The Netherlands
citations of the Rietveld method
micro-computers
(2016)
“A reasonably good starting structural model is necessary, as
Rietveld Refinement is not a resolution method“ (H. Rietveld)
at the origin, the Rietveld analysis was only a method for refining a crystal structure, not for solving it
!

## Slide 4
1- the FullProf suite: basic functions
what do we need before running ?
- a diffraction data file (xy, uxd, dat, xrdml, …) no space in title!
- a command file template (pcr) no space in title!
- the crystallographic data of the crystalline phase(s)
first steps
- plot baseline
- fill the pcr carefully with:
- header, instrumental data from another pcr file used in similar conditions
- crystal data blocks of the phases data bases, webmineral.com, …
- refine relevant variables stepwise
running modes
- Rietveld mode: intensities are calculated from Fhkl depend on atomic positions
- Le Bail’s variant: only lattice and profile data are processed no need of a structure model
yi calc
yi obs
yi obs - yi calc
Bragg_pos.

## Slide 5
title
number of crystalline phases (= n of data blocks)
number of background points
Res = 1 if a resolution function is used
Res = 0 otherwise
data file format
Ins = 9 for uxd
Ins = 10 for xy (ID22)
Ins = 13 for xrdml (PanAlytical)
…
name of data file
(place in same folder)
name of resolution file
if Res = 1 (option)
(place in same folder)
number of cycles per run
χ2 = goodness of fit
if χ2(cycle n+1) > χ2(cycle n)
WARNING = PCR is not rewritten!
wavelength(s)
Iα1 / Iα2 for Kα doublet
upper 2θ limit for asymmetry
Ilo = 0 for reflection (Bragg-Brentano)
Ilo = 3 for transmission (ID22)
dampening factors: atomic, anisotropic displacement, profile and general parameters
limit angle for full sample illumination
(Bragg-Brentano, otherwise = 0)
number of excluded regions
cos2(2θ) polarization of monochromator
0.9870 on ID22 (0.354176 Å)
0.7900 for CuKα
2- the PCR file (1/3)

## Slide 6
data block
for phase #1
(2θ, i) background coordinates
code for variable # 36, refined at 100 %
low- and high 2θ limits of excluded region # 1
automatic!
2θ zero shift
phase name
number of independent atoms
job type: 0 for Rietveld, 2 for Le Bail
0 if Jbt = 0
reset to 0 for 1st run if Jbt = 2
profile function
7 for TCH
5 for split Pseudo-Voigt
hkl of preferred orientation (Bragg-Brentano)
2- the PCR file (2/3)

## Slide 7
space group symbol
data block
for phase #1
atom name (any), ex. O1, Ow, …
element (O, strictly)
isotropic atomic displacement factor
occupancy factor
= atom multiplicity / space group order
codes for variables
scale factor
width parameters for TCH
cell parameters (Å, °)
asymmetry correction at low angle
(< ASYLIM)
2- the PCR file (3/3)

## Slide 8
3- specific settings of the pcr file for ID22
header
- Ilo = 4 transmission geometry
- Res = 0 unless using a resolution file (not detailed in this training)
- Ins = 10 xy data file format
- Lambda 1 & 2 = 0.354205 Å to be cheched
- CTHM = 0.9870 cos2(2θ) polarization of monochromator (invariant)
- AsyLim = 25 upper 2θ limit for asymmetry
- Sent0 = 0 does not apply
phase data block (to be refined)
- GauSiz = 0.00002 instrumental Gaussian width (Si standard)
- NPR = 7 Thompson-Cox-Hastings profile function
- Asy1 = Asy2 = 0.01 peaks asymmetry correction
to be introduced and refined later
- V = 0.00001 coef of tan θ for in peaks width development
- LorSiz = XXX Lorentzian size broadening depending on model (use EdPCR)

## Slide 9
3- make your own data block (ex.: hydrocerussite)
space group symbol
separate independent directions
ex. C 2/m, P n a 21, I 41/a m d, R -3 c, …
anisotropic atomic displacement factors (heavy atoms)
ex. for hydrocerussite:
order of space group R-3m is 36 (mult of xyz position)
- Pb1 occupies site 6c fully: occ = 6 x 1 / 36
- Pb2 occupies site 18c at 1/6: occ = 18 x 1/6 / 36
- O1 occupies site 18c fully: occ = 18 x 1 / 36
isotropic atomic displacement factors
to convert from U: Biso = 8π2 Uiso
occupancy
= site multiplicity x occupancy factor / space group order
for other space groups, see: https://www.cryst.ehu.es/cgi-bin/cryst/programs/nph-wp-list

## Slide 10
the truncation of the Fourier transform becomes visible
for L < 1 μm
 the reciprocal lattice points spread
 the diffraction peaks broaden
Scherrer formula 
L and λ in same unit
4- size / strain analysis
the strain of the crystal cell can be of various origins:
external: mechanical strain, quenching, lamination, forging, …
internal: chemical substitutions, defects (vacancies, interstitials, dislocations, …)
ex.: (Ba0.9Eu0.1)MgAl10O17 solid solution
rBa2+ = 1.61 Å rEu2+ = 1.44 Å  variations in the cell parameters
Bragg’s law (dif-log)  d = Δ2 (rad) = 4ε tan ε = Δd/d: strain coefficient
strain-induced broadening (d)
size-induced broadening (L)
K
1 a*
2 a*
3 a*
N = 5
N = 10
N = 20
N = ∞
diffracted intensities around lattice points h00

## Slide 11
4- size / strain analysis
the Williamson-Hall analysis
 = 4 ε tan + 0.9 λ/L cos
  cos = 4 ε sin + 0.9 λ/L
sin
.cos
0.9. λ/L
4 ε
0
linearization allows to discriminate size and strain effects
ex.: Williamson-Hall plot for hydrocerussite sampled on a Claude Monet painting
(La Cathédrale de Rouen, le Portail et la Tour Saint-Romain, 1893, Musée d’Orsay)
ID22
λ = 0.3547 Å
- the instrumental function is required (Si or LaB6 pattern)
- peaks FWHM can be collected from the hkl output file (if the fit is good), or measured one by one using Calculation / Profile fitting
- otherwise, the instrumental function can be directly implemented in FullProf
operating modes
 corresponds to the broadening measured on the integral width:  = √(exp2 - ins2)

## Slide 12
4- size / strain analysis
application to ultramarine (from Alessa Gambardella’s post-doc work at the Rijksmuseum)
Through a Williamson-Hall analysis, we will try to assess the effect of the heat treatment at 750 °C of an ultramarine sample (7 phases identified) on the microstructure of the main lazurite phase.
The zeolitic cages (below) contain several species (S2-, S22-, SO42-, H2O, …). What will become of them at HT is hard to measure by XRD due to high disorder, but the effect of the heat treatment on the microstructure can give precious information.

## Slide 13
5- semi-quantitative analysis
What was the chemical composition of the pigments used by these Renaissance masters? Identify all the visible phases and determine the pigments’ compositions through Rietveld analysis.
The relative amounts of the crystalline phases, computed from their scale factors, are reported at the end of sum output file.
The Holy Family
Raffaello (1518)
Musée du Louvre
Portrait of the Marquise of Santa Cruz
Francisco de Goya (1798-1799)
Musée du Louvre
application to lead white pigments (from Victor Gonzalez’s PhD work at the C2RMF)
Mona Lisa
Leonardo da Vinci (1516?)
Musée du Louvre
Portrait of Maerten Soolmans
Rembrandt van Rijn (1634)
Rijksmuseum & Musée du Louvre

## Slide 14
6- preferred orientation effects
XRD in reflection (Bragg-Brentano) geometry can reflect the preferred orientations of crystallites with anisotropic shape.
Generally:
c >> a, b: platelets
c << a, b: needles
c*
K = (S – So) / λ = ha* + kb* + lc*
So
S
March-Dollase modified correction function
Phkl = G2 + (1 - G2) x [(G1 cos δ)2 + sin2 δ / G1]-3/2
or more simply (Nor = 1) Phkl = [(G1 cos δ)2 + sin2 δ / G1]-3/2
+
=
c*
G2
1 - G2
G1: anisotropy
δ = ([hkl]*, c*)
c*
how to…
- measure / correct the effect: use Nor = 1, define Pr1, Pr2, Pr3 (= c* vector), then refine Pref1
- avoid preferred orientation: mix sample with amorphous, X-ray transparent powder (Nescafé, …)